Material Selection. Temperature Range; Material Bolt/ Nut. 100°C - 200°C; A320B8/Gr .8. 46°C - 100°C; A320L7/Gr .4. 0°C - 45°C; A320L7/Gr .4 SNB7/S45C. 0°C - 300°C; A307 SS400. 300°C - 400°C; A193B7/Gr .2H B7/2H SNB7/S45C. 400°C - 550°C; A193B16/Gr .4.; Temperature Range; Material Bolt/ Nut. 550°C - 650°C; A193B8/Gr .8. A193B8M/Gr .8M. 650°C; A453Gr.660, A453Gr.660/Gr 8C. 750°C; Hastalloy B & C. 1000°C; Chromium Alloy..

High Temperature High Tension Alloy Bolt Material Chemical & Mechanical Requirements ASTM A193 B7 (Cr- Mo AISI 4140,4142,4145 ) This material is considered as the most suitable for bolts to be used at temperature below 450 °. C, with a minimum effect on its structural strength during application at a high temperature. The material has the following chemical properties and physical Characteristics.

C; Mn; P; S; Si; Cr; Mo. 0.37-0.49; 0.65-1.10; 0.035 Max; 0.04 Max; 0.15-0.35; 0.75-1.20; 0.15-0.25. Dia; Minimum Tempering Temperature ( ° F ); Tensile Strength min, ksi ( MPa); Yield Strength. min, 0.2% offset, Ksi ( MPa); Elongation in 4D min %; Reduction of Area min %; Hardness max. 21/2" and under; 1,100 (593 ° C ); 125(860); 105(720); 16; 50; 321HB or 35 HRc. over 21/2" to 4"; 1,100 (593 ° C ); 115(795); 95(655); 16; 50; 302HB or 35 HRc. over 4" to 7"; 1,100 (593 ° C ); 100(690); 75(515); 18; 50; 277HB or 29 HRc.

ASTM A1193 B7M (Cr- Mo AISI 4140,4142,4145 )

C; Mn; P; S; Si; Cr; Mo. 0.37-0.49; 0.65-1.10; 0.035 Max; 0.04 Max; 0.15-0.35; 0.75-1.20; 0.15-0.25. Dia; Minimum Tempering Temperature ° F (°C); Tensile Strength min, ksi MPa; Yield Strength. min, 0.2% offset, Ksi; Elongation in 2" min %; Reduction of Area min %; Hardness max. 21/2" and under; 1150 (620 ° C ); 100(690); 80(550); 18; 50; 235HB, 99HRB.

ASTM A193 B16 (Cr- Mo -V ) This material is considered as the most suitable for bolts to be used at temperature below 450 °. C,even at a high temperature range, the material has superior physical characterestics compared to ASTM A193 B7 previously mentioned. The chemical properties and physical characteristics are as follows

C; Mn; P; S; Si; Cr; Mo; Al; V. 0.36-0.47; 0.45-0.70; 0.035 Max; 0.04 Max; 0.15-0.35; 0.80-1.15; 0.50-0.65; 0.015Max; 0.25-0.35. Dia; Minimum Temperature ° F (°C); Tensile Strength min, ksi ( MPa); Yield Strength. min, 0.2% offset, Ksi ( MPa); Elongation in 4D min %; Reduction of Area min %; Hardness max. 21/2" and under; 1200(650); 125(860); 105(725); 18; 50; 321HB or 35 HRC. over 21/2" to 4"; 1200(650); 110(760); 95(655); 17; 45; 302HB or 33 HRC. over 4" to 7"; 1200(650 ); 100(690); 85(586); 16; 45; 227HB or 29 HRC.

ASTM A193 B5 (5% Cr AISI 501)

C; Mn; P; S; Si; Cr; Mo. 0.10 max; 1.00 max; 0.040 max; 0.030 Max; 1.0 Max; 4.00 - 6.00; 0.40 -0.65. Dia; Minimum Tempering Temperature ° F (°C); Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. up to 4" incl; 1.100 (593 ); 100(690); 80(550); 16; 50; -.

ASTM A193 B8 (AISI 304) B8A Chemical Requirements

C; Mn; P; S; Si; Cr; Ni. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 18.00 - 20.00; 8.00 -10.50.

ASTM A193 B8C (AISI 347) B8CA

C; Mn; P; S; Si; Cr; Ni; Columbium + Tantalum. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00 - 19.00; 9.00 -13.00; 10 x Carbon content, min.

ASTM A193 B8N (AISI 304N) B8NA

C; Mn; P; S; Si; Cr; Ni; Nitrogen. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 18.00 - 20.00; 8.00 -10.50; 0.10 - 0.16.

ASTM A193 B8MN (AISI 316N) B8MNA

C; Mn; P; S; Si; Cr; Ni; Mo; Nitrogen. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 16.00 - 18.00; 10.00 -14.00; 2.00 - 3.00; 0.10 - 0.16.

ASTM A193 B8P (AISI 305) B8PA

C; Mn; P; S; Si; Cr; Ni. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00 - 19.00; 10.50 -13.00.

ASTM A193 B8T (AISI 321) B8TA

C; Mn; P; S; Si; Cr; Ni; Titanium. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00 - 19.00; 9.00 -12.00; 5 x Carbon content, min.

ASTM A193 B8R B8RA

C; Mn; P; S; Si; Cr; Ni; Mo; Nitrogen; Columbium + Tanalum; V. 0.06 Max; 4.00 - 6.00; 0.040 Max; 0.030 Max; 1.00 Max; 20.50 - 23.50; 11.50 -13.50; 1.50 - 3.00; 0.20 - 0.40; 0.10 - 0.30; 0.10 - 0.30.

ASTM A193 B8S B8SA

C; Mn; P; S; Si; Cr; Ni; Nitrogen. 0.10 Max; 7.00 - 9.00; 0.040 Max; 0.030 Max; 3.50 - 4.50; 16.00 - 18.00; 8.00 - 9.00; 0.08 - 0.18.

ASTM A193 B8LN, B8LNA

C; Mn; P; S; Si; Cr; Ni; Mo; Nitrogen. 0.030 Max; 2.00; 0.045 Max; 0.030 Max; 1.00; 18.00 - 20.00; 8.00 - 10.50; -; 0.10 - 0.16.

B8MLN, B8MLNA

C; Mn; P; S; Si; Cr; Ni; Mo; Nitrogen. 0.030 Max; 2.00; 0.045 Max; 0.030 Max; 1.00; 16.00 - 18.00; 10.00 - 14.00; 2.00 - 3.00; 0.10 - 0.16.

CLASS I: B8, B8C, B8M, B8P, B8T, B8LN, B8MLN Mechanical Requirements

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated; 75(515); 30(205); 30; 50; 223 HB or 96HRB (3/4" in & smaller, 241HB or 100 HRB).

CLASS IA: B8A, B8CA, B8MA, B8PA, B8TA, B8LNA, B8MLNA, B8NA, B8MN4

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated in the finished conditions; 75(515); 30(205); 30; 50; 192 HB or 90HRB.

CLASS IB: B8N, B8MN

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated; 80(550); 35(240); 30; 40; 223 HB or 96HRB (3/4" in & smaller, 241HB or 100 HRB).

CLASS IC: B8R

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated; 100(690); 55(380); 35; 55; 271 HB or 28 HRC.

CLASS IC: B8RA

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated in the finished condition; 100(690); 55(380); 35; 55; 271 HB or 28 HRC.

CLASS IC: B8S

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated; 95(655); 50(345); 35; 55; 271 HB or 28 HRC.

CLASS IC: B8SA

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. All diameters; Carbide Solution Treated in the finished condition; 95(655); 50(345); 35; 55; 271 HB or 28 HRC.

CLASS 2: B8, B8C, B8P, B8T, B8N

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. 3/4" & under; Carbide Solution Treated and strain Hardened; 125(860); 100(690); 12; 35; 321 HB or 35 HRC. over 3/4" & 1" incl; 115(795); 80(550); 15; 35. over 1" & 11/4" incl; 105(725); 65(450); 20; 35. 11/4" to 11/2" incl; 100(690); 50(345); 28; 45.

CLASS 2: B8MN / B8M

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. 3/4" & under; Carbide Solution Treated and strain Hardened; 110(760); 95(655); 15; 45; 321 HB or 35 HRC. over 3/4" & 1" incl; 100(690); 80(550); 20; 45. over 1" & 11/4" incl; 95(655); 65(450); 25; 45. 11/4" to 11/2" incl; 95(655); 75(515); 25; 40.

CLASS 2B: B8M2

Dia; Heat Treatement; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness°max. 2" & under; Carbide Solution Treated and strain Hardened; 95(655); 75(515); 25; 40; 321 HB or 35 HRC. over 2" & 21/2" incl; 90(620); 65(450); 30; 40. over 21/2" to 3" incl; 80(550); 55(380); 30; 40.

Low-Temperature Alloy Steel Bolt Material Chemical & Mechanical Requirements ASTM A320-L7 (Cr- Mo AISI 4140,4142,4145 ) This material is considered as the most suitable for bolts to be used at temperature 0-(-)100 ° C, The chemical properties and physical characteristics are as follows:

C; Mn; P; S; Si; Cr; Mo; Impact Energy Absorption Requirements. 0.38-0.48; 0.75-1.00; 0.035 Max; 0.04 Max; 0.15-0.35; 0.80-1.10; 0.15-0.25; Minimum Impact Value; Minimum Impact Value. Dia; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max; Required for Average of Each set of three specimens ft lbf [J]; Permitted for Specimen only of a set ft lbf [J. 21/2" and under; 125 ( 860 ); 105 ( 725 ); 16; 50; 277-321HB for reference; 20[27]; 15[20].

ASTM A 320 L7M Dia.; Heat Treatment; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Reduction of Area min %; Hardness max. 21/2" and under; Quenched and tempered at 1,150 ° F (620 ° C) min; 100(690); 80(550); 18; 50; 235HB or 99HRB. ASTM A320 B8 (18Cr-8Ni AISI 304) This material is considered as the most suitable for bolts and nuts to be used at temperatures (-)100-(-)200 ° C The chemical properties are as follows: C; Mn; P; S; Si; Cr; Ni. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 18.00-20.00; 8.00-10.50. ASTM A320 B8M C; Mn; P; S; Si; Cr; Ni; Mo. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 16.00-18.00; 10.00-14.00; 2.00-3.00. ASTM A320 B8C C; Mn; P; S; Si; Cr; Ni; Columbium + Tantulum. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00-19.00; 9.00-13.00; 10 * Carbon content, min. ASTM A320 B8T C; Mn; P; S; Si; Cr; Ni; Titanium. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00-19.00; 9.00-12.00; 5 * Carbon content, min. Super High Temperature Resistant Bolt Material Chemical & Mechanical Requirements This material is considered as suitable for bolts to be used as temperature below 1,200 ° F (650 ° C) and the material has superior resistence to oxidation and shrinkage to those high temperature resistant bolt material mentioned so far. The chemical properties and physical characteristics are as follows: ASTM A453 Gr. 660 C; Mn; P; S; Si; Cr. 0.08 Max; 2.00 Max; 0.040 Max; 0.030 Max; 1.00 Max; 24.00-27.00. Cr; Mo; Ti; Al; V; Boron. 13.50-16.00; 1.00-1.50; 1.90-2.35; 0.35 Max; 0.10-0.50; 0.0010 - 0.010. CLASS; Tensile Strength min, ks (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 4x Dia. min,%; Reduction of Area min, %; Brinell Hardness Number. A,B and C; 130(895); 85(585); 15; 18; 248-341 (min 99HRB, max 37HRC). ASTM A453 Gr. 651 C; Mn; P; S; Si; Cr. 0.28 - 0.35; 0.75 -1.50; max 0.040; max 0.030; 0.30 - 0.80; 8.00-11.00. Cr; Mo; Ti; W; Cb; Cu. 18.00-21.00; 1.00-1.75; 0.10 - 0.35; 1.00 - 1.75; 025 - 0.60; max 0.50. CLASS; Tensile Strength min, ks (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 4x Dia min, %; Reduction of Area min, %; Brinell Hardness Number. A ( 3" and under); 100(690); 70(485); 18; 35; 217-277 (min 95HRB, max 28HRC). A (over 3"); 60(415). B ( 3" and under); 95(655); 60(415); 18; 35; 217-277 (min 95HRB, max 28HRC). B (over 3"); 50(345). ASTM B408 (800,800H) Ni; Cr; Fe; Mu; C; Cu; Si; S; Al; Ti. 30.0 - 35.0; 19.0 - 23.0; *39.5 min; 1.5 Max; 0.10 Max; 0.75 Max; 1.0 Max; 0.015 Max; 0.15 - 0.60; 0.15 - 0.60. * = Iron shall be determined arithmetically by differenece CLASS; CONDITION; Tensile Strength min, ksi (MPa); Yield Strength. min, Ksi (MPa); Elongation in % min. 800; (all sizes) Hot finished rods and bars; 80(550); 35(240); 25. (all sizes) Cold drawn and (annealed) Hot finished rods and bars; 75(520); 30(205); 30. 800H; (all sizes) Cold drawn and (annealed) Hot finished rods and bars; 65(450); 25(170); 30. HASTALLOY C/ASME SB336,UNS N10002 Class; Ni; Co; Cr; Mo; W; Fe; Si; Mn; C. C; Balance; < 2.5; 16; 16; 4; 5; < 1.00; < 1.00; < 0.08. Monel K-500 Ni; C; Mn; Fe; S; Si; Cu; Al; Ti. 63 - 70; 0.25 Max; 1.50 Max; 2.00 Max; 0.01 Max; 0.5 Max; balance; 2.3 - 3.15; 0.35 - 0.85. Monel 400 Ni; C; Mn; Fe; S; Si; Cu. 63 - 70; 0.30 Max; 2.0 Max; 2.5 Max; 0.024 Max; 0.050 Max; balance. Nut Material Chemical & Mechanical Requirements ASTM A194 Gr.2H This is the material for bolts made from ASTM A-193 B7, considered to be used with suitable heat treatment. The chemical properties and physical characteristics are as follows : C; Mn; P; S; Si; Brinell Hardness; Rockwell Hardness. 0.40 Min; 1.00 Max; 0.040 Max; 0.050 Max; 0.40 Max; To 11/2" incl 248 to 352; 24 to 38 HRC. Over 11/2",212 to 352; 38 HRC Max. ASTM A194 Gr.2HM C; Mn; P; S; Si; Brinell Hardness; Rockwell Hardness. 0.40 Min; 1.00 Max; 0.040 Max; 0.050 Max; 0.40 Max; 159 to 237; 22 HRC Max. ASTM A194 Gr.4 This material is considered as the most suitable for nuts,when they are used with bolts made from ASTM A-193 B16 and A-320 L7. Even at high temperature range. then material has superior physical characteristics to those ASTMA A-194 2H previously mentioned. The chemical properties and physical characteristics are as follows : C; Mn; P; S; Si; Mo; Brinell Hardness; Rockwell Hardness. 0.40 - 0.50; 0.70 - 0.90; 0.035 Max; 0.04 Max; 0.15 - 0.35; 0.20 - 0.30; 248 to 352; 24 to 38 HRC. ASTM A194 Gr. 8 (AISI 304) This is nut material for bolts made from ASTM A-193 B8, considered to be used with suitable heat treatment. The chemical properties and physical characteristics are as follows : C; Mn; P; S; Si; Cr; Ni; Brinell Hardness; Rockwell Hardness. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 18.00 - 20.00; 8.00 - 10.50; 126 to 300; 60 to 105 HRB. ASTM A194 Gr. 8M (AISI 316) This is nut material for bolts made from ASTM A-193 B8M and A-320 B8M, considered to be used with suitable heat treatment. The chemical properties and physical characteristics are as follows : C; Mn; P; S; Si; Cr; Ni; Mo; Brinell Hardness; Rockwell Hardness. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 16.00 - 18.00; 10.00 - 14.00; 2.00 - 3.00; 126 to 300; 60 to 105 HRB. ASTM A194 Gr. 8C (AISI 347) This is nut material for bolts made from ASTM A-193 B8C, A-320 B8Cand A-320 B8T, considered to be used with suitable heat treatment. The chemical properties and physical characteristics are as follows : C; Mn; P; S; Si; Cr; Ni; Cb + Ta; Brinell Hardness; Rockwell Hardness. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00 - 19.00; 9.00 - 13.00; 10 * C% min; 126 to 300; 60 to 105 HRB. ASTM A194 Gr. 8T (AISI 321) This is nut material for bolts made from ASTM A-193 B8Tand A-320 B8T, considered to be used with suitable heat treatment. The chemical properties and physical characteristics are as follows : C; Mn; P; S; Si; Cr; Ni; Ti; Brinell Hardness; Rockwell Hardness. 0.08 Max; 2.00 Max; 0.045 Max; 0.030 Max; 1.00 Max; 17.00 - 19.00; 9.00 - 12.00; 5 C% min; 126 to 300; 60 to 105 HRB.

ASTM A307 This material is suitable in structural application where nominal strength alongwith weldability is required. Grade; P; S; Tensile Strength min, ksi (MPa); Yield Strength. min, 0.2% offset, Ksi (MPa); Elongation in 2" min %; Hardness max. A; 0.06 Max; 0.15 Max; 60 (415); -; 18; 121 - 241 BHN. B; 0.04 Max; 0.05 Max; 60 - 100 (415 - 690); -; 18; 121 - 212 BHN. C; -; -; 58 - 80 (400 - 550); 36(50); 23; Not Required.

ASTM A563 This specification of material is used for manufactoring nuts for balts/styds made from ASTM A307 Grade; C; Mn (Max); P (Max); S (Max). O,A,B,C; 0.58 Max; -; 0.13; -. D; 0.58 Max; 0.27; 0.048; 0.058. DH; 0.18-0.58; 0.57; 0.048; 0.058.

Grade; Hardness Required. O; 103 to 302 BHN. A; 116 to 302 BHN. B; 90 to 121 BHN. C; 143 to 352 BHN. D; 159 to 352 BHN. DH; 248 to 352 BHN.